LAMINEX TIMBER BOX CULVERT

PART 1 – GENERAL

  - SCOPE

- Design, furnish and deliver Laminex Timber Box Culvert in accordance with the requirements of the plans and specifications.

  - RELATED REQUIRED WORK

- The Manufacturer shall be responsible for designing, detailing, fabricating, and delivering components for the entire Laminex Timber Box Culvert.

  - UNIT PRICES

- Payment for “Laminex Timber Box Culvert” shall be compensation in full for all costs of design, supply, fabricating, and delivery Laminex Timber Box Culvert.

  - REFERENCES

- State of Wisconsin Department of Transportation “Standard Specifications for Highway and Structure Construction”, current edition.

- AASHTO Standard Specifications for Highway Bridges – current edition

- AWPA Standards – current edition

- NFPA 1991 National Design Specifications for Wood Construction.

PART 2 - DESIGN

2.01	LAMINEX TIMBER BOX CULVERT

- Laminex Timber Box Culvert as designed by Wheeler Lumber, LLC, or approved equal.

- Timber box shall be comprised of bolted panels field assembled to provide floor, side walls, top and partition walls of the box culvert.  All panels shall be sized and detailed based on soil cover and vehicle loading as dictated in the plans.

- Design shall be in accordance with AASHTO specifications.

- Barrel lengths as dictated on plan documents.

- Complete aprons including wings and curtain wall shall be provided at both ends of the barrel.

- Barrel ends shall be skewed in accordance with the plan documents.

PART 3 – MATERIALS

3.01	STRUCTURAL TIMBER

- This section shall include only such lumber and timber as is part of the completed work.  It shall not include falsework, forms, bracing, sheeting or other lumber and timber used for erection purposes.

- All structural timber shall be in accordance with WisDOT Section 507.

- Only pieces consisting of sound wood free from any form of decay shall be accepted.  No piece of exceptionally lightweight shall be accepted.

- Knotholes and holes from causes other than knots shall be measured and limited as provided for knots.  All visible pieces of lumber and timber having knots that are unsightly in appearance shall be rejected.  Cluster knots and knots in groups are not permitted.

- Lumber and timber meeting the requirements of Structural Timber only shall be permitted.

- All structural timber furnished shall conform to the dimensions specified for either rough or surfaced stock.

- All timber to be graded as per NFPA 1991 National Design Specifications for Wood Construction.

  - PRESERVATIVE TREATMENT

- This section covers the wood preservatives and the preservative treatment of lumber, timber, piling and posts conforming to the Specifications as referenced or otherwise specified in the plans or special provisions.

- Preservative treatment of Structural Timber and lumber shall be by the pressure process, and unless otherwise provided in the contract special provisions, be in accordance to the requirements of the specifications for Preservatives and Pressure Treatment Process for Timber, AASHTO Designation: M 133.  Unless otherwise directed by the Engineer the material shall be graded prior to treatment.  Material shall be accepted after treatment on the basis of its condition prior to treatment, on the basis of inspection of the treatment procedure substantiated by plant records, on the condition of the material after treatment and on absorption, penetration and visual inspection.

- Preservatives and Preservative Treatments shall be in accordance with WisDOT Section 507.

- So far as practicable all adazing, boring, chamfering, framing, gaining, mortising, surfacing and general framing, etc., shall be done prior to treatment.  If cut or drilled after treatment, coat cut surfaces according to AWPA M4.

- All Douglas Fir or other permissible species that are difficult to penetrate shall be incised prior to treatment.

- All timber to be pressure treated with Copper Naphthenate.

  - HARDWARE

- All hardware (machine bolts, carriage bolts, drift pins, lag screws, dowels, rods, nails, spikes, washers, connectors, etc.) shall be hot-dipped galvanized and shall conform to WisDOT Section 507.

- Unless a Dome Head Bolt or approved equal is used, all bolt heads or tightening nuts in contact with Structural Timber and lumber shall have a washer of sufficient thickness and bearing area to ensure a minimum deformation of the contacted surface when tightened to develop not more than the maximum allowable tensile stress of that bolt.

- Bolt heads or tightening nuts in contact with metal surfaces shall have a cut washer or approved equal placed between the bolt head or nut and the metal surface.

# PART 4 – SUBMITTALS

  - SEALED PLAN

- A detailed representative plan shall be included with the bid proposal. Culvert plans, specific to the site and in compliance with these specifications, sealed by a professional engineer registered in the State of Wisconsin and experienced in timber culvert design, shall be submitted to the Owner within 2 weeks after award of contract.  The culvert plan shall include all details necessary for the construction of the Laminex Timber Box Culvert.  Detailed shop drawings shall be submitted to Owner prior to fabrication.

- Materials to be delivered to jobsite 8-12 weeks after approval of plan.

  - TIMBER CERTIFICATION

- The manufacture shall submit a certificate of compliance to the provisions of WisDOT Section 507 for all timber incorporated into the structure upon completion of delivery of all items deemed his responsibility by way of the bid.

- The manufacture shall be regularly engaged in the production of the specified product or item and be able to furnish independent records or references of competence and satisfaction of this fact upon the request of the Owner.

# PART 5 – QUALITY ASSURANCE

  - MANUFACTURE

- All material shall be well manufactured.  All lumber and timber shall be straight, well sawed, sawed squared at ends and have opposite surfaces parallel unless otherwise required by the plans and specifications.

- Box panels shall be assembled with 3/8” diameter threaded rods.

- Box panels to be delivered to jobsite after being fully assembled at fabrication plant.

  - WORKMANSHIP

- Workmanship shall be first class throughout.  Nails and spikes shall be driven with sufficient force to set the heads flush with the surface of the wood, thus ensuring the surface shall be free from deep or frequent hammer marks.

  - HANDLING

- Lumber and timber shall be handled with sufficient care to avoid breaking through portions penetrated by treatment, and thereby exposing untreated wood.  Chains, peavies, cant hooks, pickaroons, timber dogs, pike poles and other pointed tools that would burr, blemish, penetrate or permanently deform the contacted member shall not be used.  Rope, rubber or fabric slings only shall be used.