COPPER NAPHTHENATE SPECIFICATION

# PRESERVATIVE TREATMENT

- This section covers the wood preservatives and the preservative treatment of lumber and timber conforming to the Specifications as referenced or otherwise specified in the plans or special provisions.  Temporary bracing shall not require preservative treatment.

- Preservative treatment of lumber and timber shall be by the pressure process, and unless otherwise provided in the contract special provisions, be in accordance AWPA Standards and AASHTO Designation M 133.

- Lumber and timber specified in the plans or special provisions to be treated with Copper Naphthenate in AWPA P9 Type A Hydrocarbon Solvent.

- Unless otherwise directed by the Engineer the material shall be graded prior to treatment.  Material shall be accepted after treatment on the basis of its condition prior to treatment, on the basis of inspection of the treatment procedure substantiated by plant records, on the condition of the material after treatment and on absorption, penetration and visual inspection.

- So far as practicable all adazing, boring, chamfering, framing, gaining, mortising, surfacing and general framing, etc., shall be done prior to treatment.  If cut after treatment, coat cut surfaces according to AWPA M4.

F.	All Douglas Fir and other species that are difficult to penetrate shall be incised prior to treatment.